GUIDELINES – Use when requested by the Designer for asphalt projects. {2007-S315AA0}

SP211-000400-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

COLD CENTRAL PLANT RECYCLING MATERIAL

August 7, 2015; Reissued July 12, 2016

I.	DESCRIPTION

These specifications cover the requirements for Cold Central Plant Recycling Material (CCPRM).  Cold Central Plant Recycling (CCPR) is a process in which recycled asphalt concrete pavement is processed and stabilized using foamed asphalt or emulsified asphalt at a plant and then placed using conventional asphalt paving equipment.  CCPRM shall not be used as a final riding surface.

II.	MATERIALS

1.	Stabilizing Agent (Emulsified or Foamed Asphalt) – All liquid asphalts used for stabilizing agents shall be emulsions or PG binders (List Nos. 50 and 50.1) on the VDOT Materials Division’s Approved List.  Emulsified asphalts shall conform to Section 210 of the Specifications; liquid asphalts shall be a neat (i.e., not modified) asphalt that meets Section 211.02 of the Specifications.

2.	Water – Any water used for mixing shall meet Section 216 of the Specifications.

3.	Crushed Reclaimed Asphalt Pavement (RAP) Material – RAP material shall meet Section 211.02(j) 4. of the Specifications and TABLE 1 herein.

| TABLE 1 CRUSHED RAP PROPERTIES |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Deleterious Materials: Clay Lumps and Friable Particles in Aggregate | AASHTO T 112 | 0.2% maximum |
| Maximum Sieve Size, 1.5 inches (37mm) | AASHTO T 27 | 100% Passing, |

4.	Aggregate – Based on the results of the job mixture design(s) or other requirements of this provision, the Contractor shall determine if additional aggregate is required.  If the Contractor determines additional aggregate is needed any additional aggregate shall meet Section 203 of the Specifications and TABLE 2 herein, and it shall be graded to produce a product which meets the specification requirements given in TABLE 3.  The percentage of additional aggregate used in the mixture shall not exceed 50 percent.

5.	Other Additives – If necessary, additional additives may be used to meet the requirements in TABLE 4.  In the case where an additional additive is used, the type and dosage must be described in the Job Mix Formula(s) submitted to the Department.

| TABLE 2 AGGREGATE PROPERTIES |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Los Angeles Abrasion Value | AASHTO T 96 | 45% maximum loss |
| Sand Equivalent | AASHTO T 176 | 45% minimum |
| Maximum size, 100% Passing, Sieve Size | AASHTO T 27 | 1.5 inches (37mm) |
| Water absorption | AASHTO T 85 | 3% maximum |

III.	Job-Mix Formula

A job-mix formula (JMF) for CCPRM shall be submitted to the Engineer for approval no less than 30 calendar days prior to the start of CCPRM operations.  More than one JMF may be required.  The gradation of each JMF shall fall within the bands shown in TABLE 3.  If gradation fails to meet the requirements, the Department at its discretion reserves the right to require appropriate measures that may include stopping the work.

| TABLE 3 CCPRM DESIGN RANGE |  |  |
| --- | --- | --- |
| Sieve Size | Percentage by Weight Passing Square Mesh Sieves (in) |  |
|  | Lower | Upper |
| 1.5” | 100 | 100 |
| 3/4" | -- | -- |
| 3/8” | -- | -- |
| No. 4 | -- | -- |
| No. 200 | 2 | 9 |

Values based on AASHTO T 27 using washed, pulverized materials, prior to stabilization.

For CCPRM using Foamed Asphalt, cement can be used as a portion of the material passing the No. 200 sieve.

The Contractor shall establish, as part of the JMF, a target percent passing for the 1.5”, 3/4", 3/8”, No. 4 and No. 200 sieves.  The JMF(s) shall be created using either existing materials obtained directly from the project site (prior to the start of construction) or from an existing stockpile of Reclaimed Asphalt Pavement (RAP).  Sampling shall be conducted at a maximum of once per 2500 lane-feet when sampled from the road.  When sampling from a stockpile, material shall be taken from various locations around the stockpile and combined to produce a representative sample.  Each JMF shall provide as a minimum the following mix design parameters:

1)	Target field density,

2)	Percent by weight of all stabilizing agent(s) to be added to the recycled mix,

3)	Percent by weight of water (at room temperature) required,

4)	Expansion ratio and half-life characteristics and temperature of asphalt binder at the time of dosage into foaming chamber (for mixtures using foamed asphalt), minimum curing time/set time for the emulsified asphalt and temperature of emulsified asphalt at the time of dosage into the mixture (for mixtures using emulsified asphalt), and

5)	Target gradation for sieve sizes 1.5”, ¾”, 3/8”, No. 4 and No. 200 (including any aggregate to be added).

If a change in source materials is made during construction, the Contractor shall create a new JMF(s) and submit it to the Engineer for approval prior to use.  The JMF(s) shall meet the criteria of Table 4 at the approved stabilizing agent(s) content.

| TABLE 4 CCPRM MIX DESIGN CRITERIA |  |  |  |
| --- | --- | --- | --- |
| Item | Test Method | Criteria | Fabrication / Conditioning Procedure |
| Emulsified Asphalt Stabilized Materials |  |  |  |
| 1 | Moisture Density Relations AASHTO T 180, Method D | Determined by Design |  |
| 2 | Marshall Stability Test ASTM 5581 (6 inch specimens), AASHTO T 245 (4 inch specimens) | 2500 lbs minimum (6 inch (150mm) diameter specimen), or 1250 lbs (4 inch (100mm) diameter specimen) | Three (3) specimens shall be produced at 75 blows per side (or 30 gyrations per AASHTO T 312) and cured at 140ºF (60°C) to constant mass, hold specimens at 104ºF (40°C) for 2 hours in a forced draft oven immediately prior to testing. |
| 3 | Retained Stability ASTM 5581 (6 inch specimens), AASHTO T 245 (4 inch specimens) | 70% of results of #2 | An additional three (3) specimens shall be produced at cured at 140ºF (60°C) to constant mass. Specimens shall then be vacuum saturated to 55-65%, 77ºF (25°C) water bath for 23 hours and 104ºF (40°C) water bath for an additional hour immediately prior to testing |
| 4 | Raveling Stability (ASTM D 7196) | Maximum 2% | Specimens shall be produced using a gyratory at 20 gyrations and cured at 50ºF (10°C) for 4 hours at 50% humidity. |
| 5 | Thermal Cracking (Indirect Tensile Test, AASHTO T 322) | The critical cracking temperature must be less than or equal to the pavement temperature given for the project climate area and pavement depth by LTPPBind. | See Notes 1 through 7 below. |
| Foamed Asphalt Stabilized Materials |  |  |  |
| 1 | Moisture Density Relations AASHTO T 180, Method D | Determined by Design |  |
| 2 | Dry Indirect Tensile Strength (ITS), AASHTO T 283 Section 11 | 45 psi minimum | Three (3) specimens shall be produced using 75 blows per side (or 30 gyrations per AASHTO T 312) compacted at or below OMC and cured as follows: 4 inch (100 mm) diameter specimens, oven dry at 104ºF (40°C) for 72 hrs and cool to ambient temperature for 24 hrs; 6 inch (150 mm) diameter specimens, air dried for 24 hours, then an additional 48 hours at 104ºF (40ºC) in sealed plastic bag, cool to ambient temperature for 24 hrs. |
| 3 | Retained Indirect Tensile Strength, AASHTO T 283 Section 11 | Minimum, 70% of the Dry ITS | An additional three (3) specimens shall be produced and cured according to Item 9, and then submerged in 77ºF (25ºC) water bath for 24 hours prior to testing. |
| 4 | Expansion Ratio. Wirtgen 2012 Cold Recycling Manual | 10 times when Aggregate Temperature is 50ºF to 77ºF (10 ºC to 25 ºC) 8 times when Aggregate Temperature is greater than 77ºF (25 ºC) |  |
| 5 | Half-Life – Wirtgen 2012 Cold Recycling Manual | 6 second minimum |  |
| All materials (emulsified asphalt and foamed asphalt) shall be controlled following Item 1. |  |  |  |
| 1 | Materials Gradation Test (AASHTO T 27), prior to stabilization | Gradation to control field production. |  |
| Notes: 1. Specification temperature shall be chosen using current FHWA LTPPBind software, using the weather station closest to the project. The required temperature shall be the coldest temperature at the top of the recycled layer, using 98% reliability. 2. Samples shall be compacted to 150 mm diameter and at least 115 mm height, compacted to within 1% of design air voids at the design stabilizing agent content. Compacted samples shall be cured at 140ºF (60 ºC) no less than 48 hours. Before testing, sample mass shall be checked every two (2) hours until change in mass between successive checks does not exceed 0.05%. After curing, two specimens shall be sawcut from each compacted sample to 50 mm in height. Perform bulk density testing after sawcutting. 3. Three specimens are required at each of the three (3) testing temperatures. 4. Select two testing temperatures that bracket the specification temperature above. For example, if the specification temperature is -13ºF (-25 ºC), then two of the selected testing temperatures shall be -4ºF and -22ºF (-20 ºC and -30 ºC). A temperature of 14ºF or -40ºF (-10 ºC or -40 ºC) shall be used as the third testing temperature. 5. The tensile strength test shall be performed on each specimen directly after the tensile creep test (at the same temperature as the creep test). 6. The critical cracking temperature is defined as the temperature at the intersection of the thermal stress curve (derived from the creep data) and the tensile strength line (the line connecting the average tensile strengths at the three testing temperatures). 7. To meet this specification, the critical cracking temperature predicted by the Indirect Tensile Test must be less than or equal to the pavement temperature given for the project climate area and pavement depth by LTPPBind. |  |  |  |

IV.	QUALITY CONTROL PLAN

The Contractor shall be responsible for developing and implementing a Quality Control Plan to ensure that operational techniques and activities are controlled to provide a homogeneous and finished material of acceptable quality meeting this provision.  Contractor sampling and testing shall be performed to control the processes and ensure material compliance with this special provision.  The Contractor shall provide the Quality Control Plan (according to this special provision) and Job Mix Formula(s) to the Department for approval no less than thirty (30) calendar days prior to the start of CCPRM operations.

For each CCPRM project, a project specific Quality Control Plan is required, and shall include the following (minimum) information:

1.	A description of the Contractor’s Quality Control organization, including the number of full-time equivalent employees or Sub-Contractors with specific Quality Control responsibilities, including an organizational chart showing lines of authority and reporting responsibilities.

2.	A listing by discipline with the name, qualifications, duties, responsibilities and authorities for all persons proposed to be responsible for Construction Quality Control.

3.	A Quality Control Sampling, Testing and Analysis Plan with methods that include a description of how random locations for testing and sampling are determined;

4.	Identification and description (including any accreditation) of the laboratory(s) to be used for each type of testing.  Lab shall meet Section 106.07 of the Specifications.

5.	Specify documentation for Quality Control activities;

6.	Procedures to meet contract requirements for corrective action when Quality Control criteria are not met.

7.	Procedures to protect stabilized material from receiving excessive moisture from weather events (i.e. rain, fog, etc.) and corrective actions when criteria are not met.

8.	Contingency Plan including:

(1)	Inclement weather

(2)	Equipment breakdowns

(3)	Materials shortages

(4)	Deficient density of installed CCPRM

(5)	Material doesn’t break or cure in timely manner

(6)	Gradation is outside tolerance(s)

(7)	Production modifications based on changes in ambient and/or material temperature.

V.	ACCEPTANCE

1.	Gradation – CCPRM acceptance for gradation will be based on a mean of the results of eight tests performed on pre-stabilized samples taken in a stratified random manner from each 4,000-ton lot (8,000-ton lots may be used when the normal daily production of the source from which the material is being obtained is in excess of 4,000 tons).

A lot will be considered to be acceptable for gradation if the mean of the test results obtained is within the tolerance allowed for the job-mix formula as specified in TABLE 5.  If a lot does not conform to the acceptance requirements for gradation, the Department will determine adjustment points in conformance with Section 211.09 of the Specifications.  In addition, variability will be determined according to Section 211.09 of the Specifications.

2.	Stabilizing Agent Content – The Contractor will provide with each gradation sample, a computer printout of the stabilizing agent content percentage/rate of the plant at the time of sampling.  If the dosage rate is outside 0.20 percentage points, then paving/production shall stop and the Contractor shall take corrective measures to bring the dosage rate within tolerance of the approved JMF.  In addition, a daily summary of the stabilizing agent content percentage/rate will be provided to the Department.

3.	Moisture Content – Moisture content will be reported for each Asphalt Content test.  After drying as noted if (a) above, the following equation shall be used:

% Moisture = Original Mass – Final Mass x 100

Final Mass

4.	Marshall Stability – When emulsified asphalt is used as the stabilizing agent, acceptance for Marshall Stability will be based on results of samples taken in a stratified random manner at a frequency of at least one per day or one per 1,000 tons per mix per day if more than 1,000 tons are produced daily.  If the results are less than the established job-mix target, the following pay adjustment will be applied for the tonnage represented by the results:

| % of Job-Mix Target Marshall Stability | % of Payment |
| --- | --- |
| 99.0 to 100.0 | 100 |
| 95.0 to 98.9 | 95 |
| 90.0 to 94.9 | 90 |
| Less than 90.0* | 90% pay and Cease Production |
| * The Contractor shall immediately cease production and notify the Department when results fall below 90.0% of the approved job-mix target. The Contractor shall make any necessary corrective actions to the mix and provide verification to the Engineer that it conforms to the approved job-mix formula. Should the results fall below the minimum specified in Table 4, the material represented by the failing results shall be removed and replaced at no cost to the Department. With approval of the Engineer, subsequent paving operations can resume. |  |

5.	Dry Indirect Tensile Strength - When foamed asphalt is used as the stabilizing agent, acceptance for Dry Indirect Tensile Strength will be based on results of samples taken in a stratified random manner at a frequency of at least one per day or one per 1,000 tons per mix per day if more than 1,000 tons are produced daily.  If the results are less than the established job-mix target, the following pay adjustment will be applied for the tonnage represented by the results:

| % of Job-Mix Target Dry Indirect Tensile Strength | % of Payment |
| --- | --- |
| 99.0 to 100.0 | 100 |
| 95.0 to 98.9 | 95 |
| 90.0 to 94.9 | 90 |
| Less than 90.0* | 90% and Cease Production |
| * The Contractor shall immediately cease production and notify the Department when results fall below 90.0% of the approved job-mix target. The Contractor shall make any necessary corrective actions to the mix and provide verification to the Engineer that it conforms to the approved job-mix formula. Should the results fall below the minimum specified in Table 4, the material represented by the failing results shall be removed and replaced at no cost to the Department. With approval of the Engineer, subsequent paving operations can resume. |  |

6.	Half-Life and Expansion Ratio – The Contractor shall verify and provide reports to the Department confirming that each load of asphalt binder used for foaming meets TABLE 4.

7.	Testing Records – The Contractor shall prepare separate test reports meeting the requirements of AASHTO R 18.  Records documenting the test results from TABLE 4 shall be provided to the Engineer, unless specified otherwise.

| TABLE 5 Process Tolerance |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Tolerance on Each Laboratory Sieve and Asphalt Content: Percent Plus and Minus |  |  |  |  |  |  |
| No. Tests | 1 ½” | 3/4" | 3/8” | No. 4 | No. 200 |  |
| 1 | 0.0 | 8.0 | 8.0 | 8.0 | 2.0 |  |
| 2 | 0.0 | 5.7 | 5.7 | 5.7 | 1.4 |  |
| 3 | 0.0 | 4.4 | 4.4 | 4.4 | 1.1 |  |
| 4 | 0.0 | 4.0 | 4.0 | 4.0 | 1.0 |  |
| 5 | 0.0 | 3.6 | 3.6 | 3.6 | 0.9 |  |
| 6 | 0.0 | 3.3 | 3.3 | 3.3 | 0.8 |  |
| 7 | 0.0 | 3.0 | 3.0 | 3.0 | 0.8 |  |
| 8 | 0.0 | 2.8 | 2.8 | 2.8 | 0.7 |  |
| 12 | 0.0 | 2.3 | 2.3 | 2.3 | 0.6 |  |

VI.	TESTING

The Contractor shall perform Asphalt Content testing and report the results as extractable asphalt or weight after ignition (VTM-102).  In addition, a RAP correction factor shall be determined according to VTM-102.  For production samples, testing shall be conducted at a rate of 1 sample per 1,000 tons and the material shall be cured to constant weight in an oven at 225° F (107° C) until the weight loss in a two hour period does not exceed 0.02% by weight ( i.e., for a 5000 gram sample, the sample does not lose more than 1 gram in a two hour period).  There will be no price adjustment for asphalt content.

VII.	EQUIPMENT

1.	CCPRM Plant: The plant shall be capable of homogeneously incorporating all stabilizing agent(s) and materials up to the sizes shown in TABLE 3.  The plant shall be capable of delivering the amount of additives to within +/- 0.2% of the required amount by weight of the pulverized bituminous material, except that a capability of adding up to 5% water by weight of the pulverized bituminous material is mandatory.  Automated systems shall be used to regulate the application of stabilizing agent(s) and water and shall adjust automatically to the mass of the material being processed.  When using foamed asphalt, the plant shall also be outfitted with a test or inspection nozzle at one end of the spray bar that can produce a representative sample.  The plant shall be capable of maintaining the temperature of the liquid asphalt at a minimum of 300°F.  The plant shall be equipped with the means for the operator to verify the stabilizing agent(s) and water are being evenly distributed and that the correct dosage rates of each are being applied.  The plant shall have the ability to print out stabilizing agent(s) and water quantities used during production.  The equipment shall be operated according to the manufacturers’ recommendations.

2.	Plant Scales:  Scales shall be approved according to Section 109.01 of the Specifications.

3.	Trucks, Truck Scales and Automatic Printer System:  Shall conform to Section 109.01 of the Specifications.