GUIDELINES – Asphalt surface treatment projects.  Include the following in the proposal: SP314-000100-00.{2007-S312CM1}

SP314-000110-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

BLOTTED SEAL COATS

August 22, 2008c; Reissued July 12, 2016

I.	DESCRIPTION

This work shall consist of application of asphalt surface treatment according to this provision and in conformity with the line and grades indicated in the Contract or designated by the Engineer.

Type B Blotted Seal is defined as two applications of liquid asphalt material, one application of cover aggregate and one application of blot fine aggregate.

Type C Blotted Seal is defined as three applications of asphalt material, two applications of cover aggregate and one application of blot fine aggregate.

Type D Blotted Seal is defined as four applications of asphalt material, three applications of cover aggregate and one application of blot fine aggregate.

II.	MATERIALS

Liquid asphalt materials shall conform to Section 210 of the Specifications.

Cover aggregate shall conform to Section 203 of the Specifications.

Fine aggregate for blotting shall conform to Section 202 minimum Grading B of the Specifications except that material shall have no more than 5 percent passing the 200 sieve by washing.

III.	APPLICATION

Application rates for asphalt and aggregate material shall be as indicated in the Contract.  These rates of application are approximate only and such rates may be altered at the direction of the Engineer.  During application, liquid asphalt material shall be maintained between 160 to 175 degrees F.  Cover material shall be applied to a complete coverage of only one aggregate depth over the treated surface.

IV.	PROCEDURES

Procedures shall be according to the Asphalt Surface Treatment special provision and the following provisions:

Each coat of liquid asphalt material shall be applied to existing surface and immediately followed by an application of aggregate.

Aggregate shall be rolled one pass immediately with a self-propelled steel wheel roller.  The roller weight shall be between 6 and 8 tons for tandem type and between 8 and 10 tons for the three wheel type.

Blot coat shall be applied with a self-propelled aggregate spreader of approved design and shall be rolled one pass immediately with a self-propelled roller.

V.	MEASUREMENT AND PAYMENT

Blotted seal coat will be measured and paid for in square yards for type specified complete-in-place, which price shall be full compensation for furnishing and applying liquid asphalt material, cover material and blot fine aggregate, protection of treatment, rolling, brooming and for all labor, tools, equipment and incidentals necessary to complete the work.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Blotted Seal Coat (Type) | Square Yard |