GUIDELINES — Asphalt projects (Plant Mix only).  Do not use Standard Drawing WP-2 (page 303.02) unless specifically requested by the District.  Any addition or variation from this specification must be submitted to and approved by the State Materials Engineer. {2007-S315OM0}

SP315-000140-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

TRENCH WIDENING ASPHALT MIXTURES

BM-25.0(T), IM-19.0D(T) or IM-19.0A(T)

July 12, 2016

SECTION 315—ASPHALT CONCRETE PAVEMENT of the Specifications is amended as follows:

Section 315.01—Description is amended to include the following:

Certain routes in the Contract are designated to use asphalt concrete type BM-25.0(T), IM-19.0A(T) or IM-19.0D(T).  Those routes are referred to herein as trench widening routes.

Section 315.02—Materials is amended to add the following:

(f)	Trench widening route materials shall conform to Section 211 of the Specifications.  IM-19.0A shall be used for IM-19.0A(T) and IM-19.0D shall be used for IM-19.0D(T).  Where BM-25.0(T) is designated, either BM-25.0A or BM-25.0D shall be used by the Contractor.

Section 315.05(e)2 Surface, Intermediate and Base Courses is amended to include the following:

Trench Widening Routes — The minimum lift density as determined according to VTM-22 is based on the type of trench widening as defined below and specified in the Contract.  Where trench widening is 2 foot in width compaction may be performed with small single drum walk-behind rollers or other mechanical means acceptable to the Engineer at the Contractor’s discretion.

Type 1 —	Paved Shoulder Only:

Trench widening routes where the widening will serve as a paved shoulder and will not be subjected to constant traffic:  The painted edge line will not be on the trench widening.  The minimum density requirement will not be enforced.  Steel double drum rollers weighing no less than 8 tons shall perform compaction of the asphalt concrete.  No less than five passes shall be completed.

Type 2 —	Widened Travel Lane and Paved Shoulder:

Trench widening routes where the widening will serve as a wider travel lane and paved shoulder that will be subjected to traffic: The widening will not include removal of existing travel lane pavement, i.e., inside the edge line marking.  The painted edge line will be on the trench widening.  The minimum density of 91.5 percent shall be enforced.

Type 3 —	Repaired Travel Lane and Paved Shoulder:

Trench widening routes where the widening will include a portion of the existing travel lane, serve as a paved shoulder and will be subjected to traffic as a part of the travel lane:  The widening will include removal of existing pavement (i.e. inside the edge line marking).  The painted edge line will be on the trench widening.  The minimum density of 91.5 percent will be enforced.

Where density requirements apply, the Contractor is responsible for cutting cores or sawing plugs for density testing.  One set of plugs/cores per course of material shall be obtained within the first 500 linear feet and every 2,500 linear feet thereafter of the trench widening route for testing by the Contractor or the Department.  Core/plug locations shall be randomly selected within each section.  If the density achieved is less than 91.5 percent for the Type 2 or 3 trench widening routes, payment will be made on the theoretical tonnage within the 500 or 2,500 linear feet lot according to Table III-5 of the Specifications.

Section 315.05—Procedures is amended to include the following:

(i)	Trench widening routes shall be widened by trenching on one or both sides of the existing roadway and placing BM-25.0(T), IM-19.0A(T) or IM-19.0D(T) commensurate with the required width and depth specified for that route.

Any remaining material, after final grading, shall be classified as excess material, and will be disposed of according to Section 106.04 of the Specifications or as directed by the Engineer.

The trench shall be shaped to have vertical sides, the width, depth and type as specified in the Contract (2-foot minimum to 6-foot maximum width), be free of excess material, and shall be tacked against the existing pavement side before BM-25.0(T), IM-19.0D(T) or IM-19.0A(T) is placed.

The Contractor shall ensure that disruption to driveways, entrances, mail boxes and intersections are minimized and that precautions are taken to ensure that roadway drainage does not pond on the roadway surface.

Section 315.08 Measurement and Payment is amended to include the following:

Asphalt Concrete Type BM-25.0(T), IM-19.0A(T) or IM-19.0D(T) will be measured in tons and will be paid for at the contract unit price per ton, which price bid shall include furnishing and placing the BM-25.0(T), IM-19.0A(T) or IM-19.0D(T) mix, trenching, tack grading and disposal of excess material.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete Type BM-25.0(T) | Ton |
| Asphalt Concrete Type IM-19.0A(T) | Ton |
| Asphalt Concrete Type IM-19.0D(T) | Ton |