GUIDELINES – For projects requiring crack sealing. {2007-S315SM1}

SP315-000200-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

SEALING CRACKS IN ASPHALT CONCRETE SURFACES OR

HYDRAULIC CEMENT CONCRETE PAVEMENT

October 19, 2014; Reissued July 12, 2016

I.	DESCRIPTION

This Specification covers the cleaning and sealing of cracks with Type A material for pavements which will not be overlaid with asphalt concrete (AC) within one year.  Type B material shall be used to fill cracks in AC surfaces or hydraulic cement pavement (HCC) joints or cracks that will be overlaid within one year.  Type C material shall be used to fill cracks in AC surfaces that may or may not be overlaid within one year.  The Contract will designate which sites are to use each material.

In addition, this Specification covers the routing (Type C only), cleaning and sealing of cracks in existing surfaces including, but not limited to, cracks along the longitudinal joint(s) between lanes.  Cracks ranging in width from 1/8 inch to 1 ½ inches shall be sealed.  Cracks that exceed 1 ½ inches are not included in this contract.

II.	MATERIALS

All sealant materials shall be certified or tested and approved by the Department before being incorporated into the work.  Where installation procedures or any part thereof are required to be according to recommendations of the manufacturer of sealant compounds, the Contractor shall submit catalogue data and copies of recommendations to the Engineer prior to installation of the materials for review and approval.  All such recommendations shall be adhered to unless directed otherwise by the Engineer.

TYPE A

The crack sealant shall be of the following type and shall meet all the requirements of ASTM D-6690 and exceed all requirements of AASHTO M-173 and Federal Specification SS-S-164:

A HOT-POURED MODIFIED ASPHALT RUBBER WITH GRANULATED CRUMB RUBBER AND LATEX PLASTICIZERS.  The proportions of the materials, by weight, shall be up to 80 percent maximum asphalt and up to 25 percent maximum crumb rubber.

The crumb rubber shall be 100 percent vulcanized rubber and meet the following gradation requirement:

| Sieve | Percent Passing |
| --- | --- |
| No. 10 | 100% |
| No. 40 | 0-40% |

TYPE B

Type B material shall consist of PG 64H-22 and polyester fibers from the Materials Division Manual of Instructions approved list of Stabilizers for Asphalt Mixtures (fibers only).  The Contractor shall provide the PG 64H-22 suppliers data for heating.  Fibers shall not exceed 5 percent by weight.  Fiber loading will be determined at the project site in order to minimize/eliminate the need for over banding as described.  The fiber loading will be approved by the Engineer.

TYPE C

Type C material shall consist of PG 64H-22 and polyester fibers from the Materials Division Manual of Instructions approved list of Stabilizers for Asphalt Mixtures (fibers only) at 5 percent by weight.  The Contractor shall provide the PG 64H-22 suppliers data for heating.

III.	EQUIPMENT

Proper sealing equipment must be used for the specific material listed according to the manufacturer's recommendations for the Sealant specified.  The equipment for hot applied sealant compounds shall be a melting kettle of double boiler, indirect heating type, using oil as a heat-transfer medium.  The kettle shall have an effective mechanically operated agitator, a re-circulation pump and shall be equipped with a positive thermostatic temperature control which shall be checked for calibration before beginning work.  The unit shall be capable of maintaining the specified mixing temperature within 10 degrees F.  Manufacturer's recommendations for mixing and application temperatures shall be followed with the latter being measured at the nozzle of the applicator wand.  Overheating or direct heating of the sealant material shall not be permitted.  The hoses, connectors and applicator wand shall all be insulated.

IV.	CONSTRUCTION

The sealant shall not be placed when the ambient or pavement temperatures fall below 45 degrees F, or when moisture is present in the crack to be sealed.

Prior to sealing, cracks shall be thoroughly cleaned as approved by the Engineer using an oil free hot air blasting heat lance capable of a velocity of 3000 fps at 3000 degrees F.  Cracks shall be cleaned such that all dirt, debris, moisture and other foreign materials that will prevent bonding of the sealant are removed to a minimum depth of 1 inch.  All foreign material (i.e., dirt, grass, rocks) shall be removed from the pavement to prevent re-contamination of the crack.  Cracks shall be completely dry before sealing.  Any crack not meeting the approval of the Engineer shall be re-cleaned and dried.

The sealant shall be pumped directly into the crack from the heater-melter unit at the temperature specified by the manufacturer immediately following the cleaning of each crack.  Cracks shall be sealed in the following manner as approved by the Engineer:

TYPE A - Cracks shall be filled from the bottom up in a continuous manner such that the crack is completely filled level with the pavement surface, and the sealant shall overlay the crack at the pavement surface leaving a maximum “over-banded" appearance of 1-inch wide on each side of the crack.  The material shall not continue to flow beyond these limits once a crack is sealed.  The height of the sealant above the pavement surface shall not exceed 1/8 inch.  For this method of sealing, the applicator wand shall be equipped with a shoe that will produce the extruded over-band as well as completely fill the crack.

TYPE B - Cracks shall be filled from the bottom up in a continuous manner such that the crack is completely filled level with the pavement surface.  The sealant may overlay the surface on each side of the by no more than ½ inch or leave a no “over-banded" appearance.  The material shall not continue to flow beyond these limits once a crack is sealed.  The height of the sealant above the pavement surface shall not exceed 1/8 inch.  For this method of sealing, the applicator wand shall be equipped with a shoe that will minimize the extruded over-band as well as completely fill the crack.

TYPE C – Prior to sealing, the cracks shall be routed to a minimum depth of 1 inch and to a minimal width of ½ inch.  Cracks shall be filled from the bottom up in a continuous manner such that the crack is completely filled level with the pavement surface, and the sealant shall overlay the crack at the pavement surface leaving a no “over-banded" appearance.  The material shall not continue to flow beyond these limits once a crack is sealed.  The height of the sealant above the pavement surface shall not exceed 1/8 inch.

Prior to the start of each day’s operation, the applicator wand and hose shall be heated per the equipment manufacturer’s recommendations and the material in the heater-melter unit re-circulated.

The applicator wand shall be returned to the mixing unit and the sealant material re-circulated immediately upon completion of each crack sealing.

Any crack in hydraulic cement concrete pavement which cannot be filled due to the sealant draining into a large void, shall be plugged with a suitable material (i.e. backer rod) approved by the Engineer prior to the project, and then filled.  After being plugged, recleaning of the crack may be required prior to filling with sealant.

During the heating and application of the crack sealing material, the temperature of the material shall be measured and recorded on two hour intervals by the Contractor.  For Type A material, the material shall never be heated over 420 degrees F.  For Type B and C material, the material shall not be heated above 375 degrees F.  Any material heated above these temperatures shall be discarded (i.e. all material in the heater-melter unit) and not paid for by the Department.  Additionally, if the material becomes lumpy or has poor flow at elevated temperature, then the material shall be discarded (i.e. all material in the heater-melter unit) and not paid for by the Department.

Traffic shall be kept off the pavement surface until the crack sealant has cured to the point it will not track or be distorted by traffic.  The Contractor shall replace, at his or her expense, any sealant that pulls out within 96 hours after opening the pavement to traffic.

V.	METHOD OF MEASUREMENT

METHOD A – CONVERSION APPROACH

Sealant for cracks or joints will be measured by the pound.  At the beginning of each workday, the Engineer, or his or her appointed representative, shall measure the amount of material in the heater-melter unit and log all additional material added during the day, and measure the amount of material remaining in the heater-melter to determine the total poundage used for that day.  No payment will be made for waste material.

For the purpose of converting the liquid material in the heater-melter unit from gallons to pounds, the Contractor shall use a calibrated measuring rod to determine the actual quantity of material in gallons, and same shall be converted to pounds taking into consideration the temperature of the material at the time of measurement.  A chart or other approved conversion method furnished by the sealant material manufacturer/supplier shall be used to perform the conversion from gallons to pounds.

METHOD B – DIRECT MEASUREMENT APPROACH

Sealant for cracks or joints will be measured by the pound.  At the beginning of each workday, the Contractor shall provide the Engineer the certified weight of the heater-melter unit.  During the day’s operation, the Engineer will log all additional material added to the heater-melter unit.  At the end of the day’s operation, the Contractor shall provide the Engineer the certified weight of the heater-melter unit including the unused material in the heater-melter unit.  The Engineer will determine the pounds of material applied for payment purposes.  No payment will be made for waste material.

VI.	BASIS OF PAYMENT

TYPE A and B

Crack Sealant/Filler will be paid for at the contract unit price per pound, which price shall be full compensation for providing the sealant/filler, complete-in-place, including cleaning and sealing the cracks and for all tools, labor, equipment, materials and incidentals related fully completing the installation.

TYPE C

Crack /Sealant/Filler will be paid for at the contract unit price per pound, which price shall be full compensation for providing the sealant/filler, complete-in-place, including routing, cleaning and sealing the cracks and for all tools, labor, equipment, materials and incidentals related fully completing the installation.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Crack Sealant/Filler (Type A) | Pound |
| Crack Sealant/Filler (Type B) | Pound |
| Crack Sealant/Filler (Type C) | Pound |