GUIDELINES — Projects requiring sealed shoulder joints. {2007-S316D00}

SP316-000110-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

SEALING SHOULDER JOINTS

August 1, 1991cc; Reissued July 12, 2016

I.	DESCRIPTION

This work shall consist of cutting a groove between pavement and shoulder surfaces according to this provision, at locations shown on the plans or as directed by the Engineer.

II.	MATERIALS

Hot-poured joint sealer shall conform to Section 212 of the Specifications.

III.	PROCEDURES

The Contractor shall construct a continuous groove by saw cutting or routing the asphalt shoulder material along the joint formed by the shoulder asphalt material and the edge of the contract paved surface.  The size of the groove after cutting and cleaning shall be at least 5/8-inch wide 5/8-inch deep having vertical sides.  The depth measurement shall be made from the surface of the shoulder or pavement, whichever is lower.  After cutting operations are completed, debris shall be promptly removed from the pavement and shoulder surfaces.

Prior to filling the groove with joint sealer, the groove shall be cleaned of all loose materials by compressed air.  The groove shall be free of dirt, dust, water, oil, grease and other materials which would prevent bonding of the joint sealer to the pavement surfaces.

At the time of placement of the sealer, the groove shall be dry and the ambient air temperature shall be at least 45 degrees F.  The groove shall be filled level with the hot pour joint sealer by means of a sealing device which will not cause air to be entraped in the groove.

IV.	MEASUREMENT AND PAYMENT

Sealing shoulder joints will be measured in linear feet, complete-in-place, and will be paid for at the contract unit price per linear foot.  This price shall include groove cutting, debris removal, groove cleaning and furnishing and placement of the hot-poured sealer.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Sealing Shoulder Joints | Linear Foot |