# GUIDELINES - For use on projects where the Plans call for use of Carbon Fiber Reinforcement Strands in Prestressed Concrete Piles.

SP405-000100-00

# VIRGINIA DEPARTMENT OF TRANSPORTATION

# SPECIAL PROVISION FOR

# CARBON FIBER REINFORCED PRESTRESSED CONCRETE PILES

December 8, 2016

SECTION 105 – CONTROL OF WORK of the Specifications is amended as follows:

Section 105.10(c)3 – Concrete Structures and Prestressed Concrete Members is amended to insert the following:

Working Drawings for concrete structures and prestressed concrete members which are reinforced with Carbon Fiber Reinforced Polymer (CFRP) tendons and other CFRP reinforcement shall provide the following, as required for the successful prosecution of the Work and which are not included in the Plans furnished by the Department: additional details related to tendon coupler locations, stressing sequence accounting for coupler locations and differing moduli of elasticity, and spacing and ties for reinforcing. All additional information shall be included in the sealed package submitted for approval.

SECTION 223 – STEEL REINFORCEMENT of the Specifications is renamed TENSILE REINFORCEMENT OF CONCRETE and amended as follows:

Section 223.02(a)8 – Carbon Fiber Reinforced Polymer (CFRP) reinforcement is inserted as follows:

Carbon Fiber Reinforced Polymer (CFRP) reinforcement shall have an ultimate tensile strength of at least 338 ksi based on the nominal area and a minimum ultimate strain of 1.30% when tested in accordance with ASTM D7205.

Section 223.02(b) – Prestressing Tendons is replaced with the following:

Prestressing Tendons, as designated on the Plans, shall be one of the following:

1.	Seven-wire, whether stress-relieved strands, stress-relieved wire, or low-relaxation strands, shall conform to ASTM A416, Grade 270; ASTM A421; and ASTM A416, Supplement I, respectively, with the following modifications:

a.	Strands or wires used in units of any one-bed layout shall be manufactured by the same plant.

b.	A manufacturer’s certification and load-elongation curve in accordance with ASTM A416 or ASTM A421 shall be obtained by the prestressed concrete fabricator for each lot of strand planned for use in fabrication.  The strand or wire manufacturer shall submit the data in permanent record form to the Engineer for approval prior to fabrication.

2.	CFRP tendons shall be from the VDOT Materials Division’s Special Products Evaluation List (SPEL).

The CFRP tendons shall have a nominal diameter as indicated on the Plans or Standard Drawings.  CFRP tendons shall be free of scoring. “Nicks” or “gouges” will not be acceptable.  Materials shall be shipped in coil form and shall be stored in such a way that kinks do not develop when the coil is unwound.  Any CFRP tendon found to be damaged on the surface, bent, subjected to temperatures above 122°F at any time, or stored out of doors shall be discarded.  A special handling guidelines manual shall be provided for CFRP tendons by the manufacturer.

SECTION 403 – BEARING PILES of the Specifications is amended as follows:

Section 403.03(b) – Precast Concrete Piles is amended by replacing the first paragraph with the following:

Precast Concrete Piles: Precast concrete piles with conventional or Carbon Fiber Reinforced Polymer (CFRP) reinforcement or tendons shall be furnished in accordance with these Specifications. Prestressed concrete piles shall be furnished in accordance with the requirements of Section 405. Piles shall be manufactured to conform to Section 404. The Class of Concrete shall be as specified on the Plans or the Specifications. If not specified, then Class A3 concrete shall be used for piles which are not prestressed.

Section 403.03(b)1 – Casting is replaced with the following:

Casting

a.	All Piles: Forms shall conform to Section 404 and shall be accessible for vibrating, tamping, and consolidating concrete. Care shall be taken to place concrete to produce a satisfactory bond with the reinforcement and avoid segregation of components, honeycombs, or other defects.

Concrete shall be continuously placed in each pile form and consolidated by vibrating. Forms shall be overfilled, the surplus concrete screeded off, and the top surface finished to a uniform, even texture similar to that produced by forms.

b.	Piles using CRFP Reinforcement:

The Contractor shall use self-consolidating concrete (SCC) conforming to Section 217.11 when using CRFP. During concrete placement, internal vibrators shall be encased with a protective polyurethane sheath.  External vibrators will be acceptable.  Extreme care shall be taken to avoid damage to CFRP tendons and reinforcement from internal vibrators.  SCC will not require any vibration; however, limited vibration that will not cause segregation may be applied to ensure flow of material in congested areas, and to provide a smooth surface.

Materials, including anchorages, couplers, and other miscellaneous hardware, shall be carefully handled to prevent any damage or deformation along the reinforcement surface, and will be stored in their original containers until required for use.  Materials, including anchorages, couplers, and other miscellaneous hardware, shall not be placed directly on the ground and shall be kept free from grease, dirt, and dust.  Any damaged material shall be removed from the final product prior to stressing. Workers shall not walk on or step on CFRP prestressing tendons during the placement of the tendons.

CFRP reinforcement shall be suitably covered to eliminate any environmental factors such as temperatures above 122°F, ultraviolet rays, and chemical substances; and shall be protected from sudden shocks or heavy hard objects and welding sparks. The CFRP reinforcement shall not be mishandled, handled in a rough manner, nor damaged (e.g. shall not be stepped on, walked on, or dragged over rough or dirty surfaces nor through rough or jagged holes in steel or wood).

CFRP reinforcement shall be properly cut to the lengths as specified on the Plans. Cutting of carbon reinforcement shall be performed by use of a high-speed rotary grinder approved by the Engineer, which will not damage the material.  Heat oriented cutting tools, such as gas welding torches, shall not be used.  Heating CFRP in any manner is dangerous and shall not be used. CFRP reinforcement shall not be field bent. Draping (harping) of tendons shall only be allowed as provided for in the Plans.

All supports, such as chairs, and tie wires shall be non-metallic material and shall not be in contact with metal reinforcement such as stainless steel. The Contractor shall use an inert, non-metallic, insulating material to prevent direct contact. All CFRP reinforcement shall be sufficiently tied down prior to placing of concrete to eliminate “floating” of reinforcement.

The Contractor shall be responsible for installing the special anchoring system on the CFRP tendons for pretensioning according to the guidelines provided by the CFRP tendon manufacturing company.  The jacking operation shall be the same as for conventional steel, except that steel transfer couplers shall be used to transfer prestressing force to the CFRP tendons. The end preparation material and steel transfer coupler shall be provided by, or approved for use with the CFRP tendon by, the CFRP tendon manufacturer.

At least 5 days prior to jacking, the Contractor shall provide the Department with PE approved shop drawings showing the CFRP tendon layout, to include coupler placement locations and offset requirements necessary to prevent collision of couplers during pretensioning due to elongation of the tendon.  The Contractor shall perform sequenced tendon jacking operations as noted on the approved Working Drawings.  The Engineer shall approve each strand force and strand elongation prior to “lock off” and jack removal.  Jacking operations shall proceed to the next strand as sequenced on the approved Working Drawings.  Steel transfer coupler shall temporarily be supported for vertical loads and prevented from any rotation movement during prestressing as noted on the approved Working Drawings.  Release of the prestressing force for anchoring shall be uniform and gradual and shall not expose any part of the pile cross section to sudden eccentric stresses.  A sudden release of pretensioning force shall not be permitted except as part of the approved detensioning process.  Release of force shall also be simultaneous at each end of the pile.  The jacking force for CFRP tendons shall be 10% greater than desired or effective prestressing force.

Section 403.03(b)2 – Curing is replaced with the following:

Curing: Steam curing will be permitted if the concrete temperature is kept below 165°F.  If CFRP is specified, the environment outside the pile where the coupler is located shall be kept below 122°F, as high temperatures will have detrimental effects on carbon reinforcement and slippage in the coupling or the anchoring.

As soon as piles have set sufficiently, side forms shall be removed and the piles moist-cured for at least 7 days.  However, if CFRP is used or the concrete piles are to be used in brackish water, tidal water, or alkali soils, the piles shall be moist-cured for at least 30 days before use. Piles shall not be driven until the concrete has reached the minimum 28-day compressive strength specified in Section 217.

SECTION 405 – PRESTRESSED CONCRETE of the Specifications is amended as follows:

Section 405.02(a) – Concrete is amended by inserting the following:

Calcium nitrite will not be required for corrosion protection in piles when Carbon Fiber Reinforced Polymer (CFRP) tendons are specified.

The Contractor shall use self-consolidating concrete (SCC) conforming to Section 217.11 when using CFRP. Vibration of SCC shall conform to Section 403.03(b)1.

Section 405.05(b) – Placing Strands and Wires and Applying and Transferring Pretension is amended to replace the sixth paragraph with the following:

The final stressing of strands shall be performed by applying tension to each strand individually or to all CFRP tendons as a group.  The strands shall be tensioned to the total pre-tensioning force as indicated on the plans, with a maximum applied stress indicated below.

| Strand Type | Percent of guaranteed ultimate strength |
| --- | --- |
| CFRP Strand | 65% |
| Stress-Relieved Strands | 70% |
| Low-Relaxation Strands | 75% |

The nominal area of the strand and reinforcing shall be confirmed between the precast concrete producer and the strand supplier.  Care shall be exercised when cutting the strand to prevent damage to the region adjacent to the cut end.

SECTION 406 – REINFORCING STEEL of the Specifications is amended as follows:

Section 406.02(e) – Carbon Fiber Reinforced Polymer (CFRP) pile confinement reinforcement is inserted as follows:

Carbon Fiber Reinforced Polymer (CFRP) pile confinement reinforcement shall be made from a product listed on VDOT Materials Division’s Special Products Evaluation List (SPEL). Ties for pile confinement shall be corrosion free.  CFRP confinement reinforcement shall have a reinforcing strength per foot which meets or exceeds the force indicated on the plans.