SQ315-000110-00

GUIDELINES — For projects with cement concrete roadways and asphalt shoulders that require patching and only asphalt material is used for the patching. {2007-SU500000A}

# VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

PARTIAL DEPTH ASPHALT PATCHING OF EXISTING CONCRETE PAVEMENT AND FULL DEPTH ASPHALT PATCHING OF EXISTING ASPHALT SHOULDERS

June 7, 2010; Reissued July 12, 2016_

I.	DESCRIPTION

This work shall consist of repairing specified sections of existing pavements by removing all or part of the defective materials in the sections and replacing them with asphalt concrete paving material.  The locations of the repairs will be specified in the Contract document and specific locations as directed by the Engineer.

II.	SCOPE OF WORK

Patching repair shall consist of the removal of areas of unsound pavement material as determined by the Engineer and replaced with asphalt concrete.

Partial Depth PCC Patching shall consist of the removal of areas of unsound PCC pavement material to a depth of no more than 50 percent of the maximum pavement thickness and replace with asphalt concrete as specified in the Contract document and as directed by the Engineer.  The pavement thickness is defined as the thickness of the Portland Cement Concrete (PCC).

Shoulder Patching shall consist of the removal of specified areas of the full thickness of the pavement section in the shoulder only to the top of the base material (bound or un-bound) and replace with asphalt concrete as specified in the Contract or as directed by the Engineer.

In the event a Shoulder Patch or Partial Depth PCC Patch fails prior to overlay, the Contractor will be responsible for removing and replacing the failed patch at no cost to the Department.

III.	MATERIALS AND EQUIPMENT

A.	Materials

All asphalt concrete shall conform to Section 211 of the Specifications and shall be IM-19.0D, unless otherwise approved by the Engineer.

B	Equipment

Saw cutting equipment shall be capable of sawing neat vertical faces along the patch boundaries.  The use of a carbide-toothed wheel saw shall not be permitted for sawing the patch boundaries in rigid pavements.  A carbide-tipped wheel saw may be used for additional saw cuts provided that a minimum 3-inch clearance from the sawed boundary is maintained.

Material in the areas identified for shoulder patching may be removed by a milling machine, backhoe, or other excavating equipment as approved by the Department.

IV.	PROCEDURES

Asphalt patches shall be placed according to Section 315 of the Specifications.  The existing pavement shall be removed with a minimum disturbance to the base material and the faces of the remaining pavement shall be cut to a smooth, vertical face without ragged edges.

The existing pavement shall be removed by milling, grinding, saw cutting or any other approved method to the specified depth for the full perimeter of the designated area.  A tack coat of CRS-2 (or other asphalt material approved by the Engineer) at a rate of 0.2 gallon per square yard shall be applied to surface and vertical faces of exposed pavement.  Exposed base material shall be primed with liquid asphalt CRS-2 at an application rate of 0.4 gallon per square yard.

PCC pavement to be removed shall be sawed along the transverse and longitudinal boundaries, including the lane and shoulder/lane joints as shown on the plans or as directed by the Engineer.  Additional saw cuts inside the patch boundaries will be permitted to facilitate the concrete removal operation.  During the removal operations, utmost care shall be exercised to minimize disturbance and damage to the reinforcing steel, and the adjacent pavement and shoulder.  Prior to application of the patch, the bottom of the excavation of all patches shall be cleaned of all loose and foreign materials.

Manual placement will be permitted for installation of the asphalt concrete.  Control strip and pavement profile measurements will be waived.  Variation between surfaces at the run on and run off joints shall not be more than 1/4 inch when tested with a 10-foot straight edge.

The existing pavement materials that are removed shall be hauled away from the repair site immediately, and disposed of properly by the Contractor according to Section 106.04 of the Specifications.

V.	MEASUREMENT AND PAYMENT

Partial Depth PCC Patching will be measured and paid for at the contract unit price per ton for the mix specified.  The payment shall be full compensation for furnishing materials and installing pavement patches complete in place.  The work shall include, but not be limited to supplying materials, saw cutting, milling, grinding, removing and disposing of existing material, the cost to haul and place asphalt concrete, and all labor, equipment, tools, supervision, fuel and incidentals necessary to complete the work.

Shoulder Patching will be measured and paid for at the contract unit price per ton for the mix specified.  The payment shall be full compensation for furnishing materials and installing pavement patches complete in place.  The work shall include, but not be limited to supplying materials, saw cutting, milling, grinding, removing and disposing of existing material, the cost to haul and place asphalt concrete, and all labor, equipment, tools, supervision, fuel and incidentals necessary to complete the work.

Main Line Patching will be measured and paid for at the contract unit price per ton for the mix specified.  The payment shall be full compensation for furnishing materials and installing pavement patches complete in place.  The work shall include, but not be limited to supplying materials, saw cutting, milling, grinding, removing and disposing of existing material, the cost to haul and place asphalt concrete, and all labor, equipment, tools, supervision, fuel and incidentals necessary to complete the work.

Liquid asphalt tack or prime will not be measured for separate payment and the cost thereof to furnish and apply the liquid asphalt shall be included in the bid price for patching.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Partial Depth PCC Patching (Asphalt Patch Mat. Type IM-19.0D) | Ton |
| Shoulder Patching (Shoulder Patch Mat. Type IM-19.0D) | Ton |
| Main Line Patching (Patch Mat. Type IM-19.0D) | Ton |