SQ315-000120-00

GUIDELINES – For projects requiring asphalt patching. {2007-SU315003A}

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

HOT MIX ASPHALT PATCHES

December 28, 2006; Reissued July 12, 2016_

I.	DESCRIPTION

This work shall consist of repairing specified sections of existing flexible or existing composite pavements by removing all or part of the defective materials in the sections and replacing them with hot mix asphalt (HMA) paving material.  The locations of the repairs will be specified in the Contract document and specific locations as directed by the Engineer.

II.	SCOPE OF WORK

Patching repair shall consist of the removal of areas of unsound pavement material as determined by the Engineer and replaced with hot mix asphalt (HMA).

III.	MATERIALS

All hot mix asphalt (HMA) shall conform to Section 211 of the Specifications.

IV.	PROCEDURES

Asphalt patches shall be placed according to Section 315 of the Specifications.  The existing pavement shall be removed with a minimum disturbance to the aggregate base material and the faces of the remaining pavement shall be cut to a smooth, vertical face without ragged edges.

The existing pavement shall be removed by milling, grinding, saw cutting or any other approved method to the specified depth for the full perimeter of the designated area.  A tack coat of CRS-2 (or other asphalt material approved by the Engineer) at a rate of 0.2 gallon per square yard shall be applied to surface and vertical faces of exposed asphalt concrete.  Exposed base aggregate shall be primed with liquid asphalt CRS-2 at an application rate of 0.4 gallon per square yard.  Where concrete is encountered prior to reaching the specified depth, the depth of the patch shall then be limited to the top elevation of the concrete.  Prior to application of the patch, the bottom of the excavation of all patches shall be cleaned of all loose and foreign materials and stabilized by hand or mechanical tamping.

Manual placement will be permitted for installation of the HMA.  Control strip and pavement profile measurements will be waived.  Variation between surfaces at the run on and run off joints shall not be more than 1/4 inch when tested with a 10-foot straight edge.

The existing pavement materials that are removed shall be hauled away from the repair site immediately, and disposed of properly by the Contractor according to Section 106.04 of the Specifications.

Minimum and maximum lift thickness for patching with HMA Superpave mixes shall be maintained during construction of the patches in conformance with the following:

| HMA SUPERPAVE LIFT THICKNESS (PATCHING) |  |  |  |
| --- | --- | --- | --- |
| MIX TYPE | MINIMUM (in.) | MAXIMUM (in.) | RECOMMENDED (in.) |
| SM-9.0 | 0.75 | 1.5 | 1.0 |
| SM-9.5 | 1.25 | 2.0 | 1.5 |
| SM-12.5 | 1.5 | 2.0 | 1.75 |
| IM-19.0 | 2.0 | 3.0 | 2.0 |
| BM-25.0 | 2.5 | 4.0 | 3.0 |

V.	MEASUREMENT AND PAYMENT

Asphalt concrete patching will be measured and paid for at the contract unit price per square yard of pavement surface for the mix and depth specified.  The payment shall be full compensation for furnishing materials and installing pavement patches complete in place.  The work shall include, but not be limited to supplying materials, saw cutting, milling, grinding, removing and disposing of existing material, the cost to haul and place asphalt concrete, and all labor, equipment, tools, supervision, fuel and incidentals necessary to complete the work.

Liquid Asphalt tack or prime will not be measured for separate payment and the cost thereof to furnish and apply the liquid asphalt shall be included in the bid price for patching.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete Patch (Depth) | Square Yard |