SQ315-000200-01

GUIDELINES – For projects where “Thin Hot Mix Asphalt Concrete Overlay” is required.{2007-SU210000B}

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

THIN HOT MIX ASPHALT CONCRETE OVERLAY

September 30, 2016_

I.	DESCRIPTION

This work shall consist of the production and placement of a thin hot mix asphalt concrete overlay according to the contract requirements, this provision, and as directed by the Engineer.

II.	MATERIALS

A.	Asphalt: The asphalt cement shall be a performance graded asphalt (PG) 64V-28 conforming to AASHTO Provisional Specification MP-1 and Section 210 of the Specifications or as designated by the Engineer

B.	RAP: Recycled asphalt pavement material will not be permitted.

C.	Coarse aggregate shall conform to Section 203 of the Specifications or as directed by the Engineer.  In addition the following requirements shall be met:

Flat and Elongated Particles when tested according to ASTM D 4791 the amount retained on and above the No. 4 sieve shall conform to the following:

3 to 1	Not greater than 25 percent.

5 to 1	Not greater than 10 percent.

Water Absorption when tested according to AASHTO T85 shall be no greater than 2 percent.

D.	Fine aggregate shall conform to Section 202 of the Specifications, except for grading, which shall be tested according to AASHTO TP 33 (Method A) with a value of not less than 45 percent and a sand equivalent value of not less than 50 (AASHTO T 176).

E.	Mineral filler shall conform to Section 201 of the Specifications.

F.	Fiber additive when required shall be cellulose or mineral fiber approved by the Engineer based on supplier’s certification of properties and documentation of success in similar applications in hot mix asphalt.

G.	Antistripping additive shall be used.  It may be hydrated lime or a chemical additive from the VDOT Materials Division Approved Products List No. 7 or a combination of both.  The approved chemical additive shall be added at a rate of not less than 0.30 percent by weight of the total asphalt content of the mixture.

The mixture shall produce a tensile strength ratio (TSR) of not less than 0.80 for the design and production tests.  The TSR shall be determined according to AASHTO T283, including a freeze-thaw cycle (4-inch specimens compacted with a Marshall Hammer or 3.5 by 6-inch specimens when compacted with a gyratory compactor); except that the 16-hour curing time requirement and the 72 to 96-hour storage period will not be enforced.by the Department.  Design tests shall use the same materials that are to be used in the production mix and shall be conducted in a laboratory approved by the Department.

When a chemical additive is used, it shall be added to the asphalt cement prior to the introduction of the asphalt cement into the mix.  Any chemical additive or particular concentration of chemical additive found to be harmful to the asphalt material or that changes the original asphalt binder performance grade (PG) shall not be used.

H.	Hydrated lime shall conform to ASTM C977.  Hydrated lime shall be added at a rate of not less than 1 percent by weight of the total dry aggregate.

A separate bin or tank and feeder system shall be provided to store and accurately proportion the dry or slurried lime into the aggregate..  The lime and aggregate shall be mixed by pugmill or other Department approved means to achieve a uniform lime coating of the aggregate prior to entering the drier.  If lime is added in dry form, the aggregate shall contain at least 3 percent free moisture.  The Department will not permit the stockpiling of lime treated aggregate.

The feeder system shall be controlled by a proportioning device, which shall be accurate to within 10 percent of the specified amount.  The proportioning device shall have a convenient and accurate means of calibration.  A flow indicator or sensor shall be provided with the proportioning device and interlocked with the plant controls, aggregate feed or weigh system, such that production of the mixture shall be consistently maintained and, if there is a stoppage of the lime feed, interrupted.

The method of introducing and mixing the lime and aggregate shall be subject to approval by the Engineer prior to beginning production.

III.	MIX FORMULA

The Contractor shall submit for the Engineer’s approval, a job mix formula within the following design ranges of percent passing each sieve size as noted:

| Sieve Size | Percent By Weight Passing Square Mesh Sieves (in) | Production Tolerance (Single Test) |
| --- | --- | --- |
| 1/2” | 100 | -2 |
| 3/8” | 85-100 | +/- 5 |
| #4 | 25-40 | +/- 4 |
| #8 | 19-32 | +/- 4 |
| #16 | 15-23 | +/- 3 |
| #30 | 10-18 | +/- 3 |
| #50 | 8-13 | +/- 3 |
| #100 | 6-10 | +/- 2 |
| #200 | 4-7 | +/- 1 |

| Asphalt Content, % | Production Tolerance (Single Test) |
| --- | --- |
| 5.0 – 5.5* | +/-0.2 |
| *Target asphalt content shall result in a minimum film thickness of 9 microns. |  |

In addition to the job mix submittal, the Contractor shall submit ignition furnace calibration data according to VTM-102 and aggregate property test results prepared by an approved testing laboratory for the aggregate components or aggregate blend.

Job mixes outside the above design range will be considered by the Engineer based on mix performance documented by the supplier to eliminate or minimize flushing or visual deficiencies and may include changes to gradation, asphalt content and/or the use of fibers.  The Engineer may require limited production of less than 300 tons for verification of an acceptable mix, prior to the Engineer’s approval of the job mix.

IV.	SURFACE PREPARATION

Prior to the commencement of paving operations, the existing pavement surface shall be cleaned of all accumulated dust, mud, vegetation or other debris, which may affect the bond of the thin lift hot mix asphalt overlay by the Contractor.

Pavement cracks or joints ¼ inch or more in width shall be cleaned and filled with a sealant material conforming to the Special Provision For Sealing Cracks in Asphalt Concrete Pavements or Hydraulic Cement Concrete Pavement.  Quantities and payment will be according to the Special Provision For Sealing Cracks in Asphalt Concrete Pavements or Hydraulic Cement Concrete Pavement.

Pavement markers, thermoplastic pavement marking and tape pavement markings shall be removed prior to the commencement of paving operations.  Pavement irregularities greater than 1 inch in depth shall be filled with a material designated in the contract or approved by the Engineer.  Payment for the material will be in according to Section 315 of the Specifications.

Utility structures shall be protected and referenced prior to paving for location and adjustment (when necessary) after paving at no cost to the Department.

V.	TACK COAT

Unless otherwise directed in the contract, two options for placing the tack coat are available.

Option 1:  A tack coat of asphalt emulsion meeting the requirements specified herein or other emulsion approved by the Engineer shall be applied prior to placement of the asphalt concrete.  The tack coat shall be placed within 10 seconds of placement of preventive maintenance asphalt concrete overlay unless otherwise directed by the Engineer.  At no time should any part of the paving machine come into contact with the tack coat before the overlay applied.  The emulsion shall be uniformly applied with a paver spray bar, except hand spray equipment may be used in areas inaccessible to the paver spray bar as directed by the Engineer inaccessible areas are exempt from the 10-second criterion.  The emulsion asphalt shall be applied at a temperature recommended by the supplier at a starting rate of 0.25 gallons per square yard +/-0.02 unless otherwise approved by the Engineer.

| Test on Emulsion | Method | Min | Max |
| --- | --- | --- | --- |
| Viscosity at 77° F, SSF | AASHTO T59 | 20 | 100 |
| Sieve Test, % (Note 1) | AASHTO T59 | — | 0.05 |
| 24 hour storage stability, % (Note 2) | AASHTO T59 | — | 1 |
| Residue from distillation at 400° F, % (Note 3) Oil portion from distillation ml of oil per 100g emulsion | AASHTO T59 | 63 | 2 |
| Demulsibility, % 35 ml 0.02 N CaCl2 or 35 ml 0.8% dioctyl sodium sulfosuccinate | AASHTO T59 | 60 |  |
| Test on Residue From Distillation |  | Min | Max |
| Elastic Recovery, % (Note 4) | AASHTO T301 | 60 | — |
| Penetration @ 77° F, 100 g, 5 sec. dmm. | AASHTO T49 | 60 | 150 |

Note 1:	The sieve test is waived if successful application of the material has been achieved in the field.

Note 2:	After standing undisturbed for 24 hours, the surface shall show no white, milky colored substance, but shall be a smooth homogeneous color throughout.

Note 3:	AASHTO T59 with modifications to include a 400° F +/- 10° F maximum temperature to be held for a period of 15 minutes.

Note 4:	With exception that the elongation is 20 cm and the test temperature is 50° F.

Option 2:  An asphalt binder tack coat meeting the requirements specified in Section 310 of the Specifications for Non-Tracking Tack Coat and listed on Approved List 50.1A shall be applied prior to placement of the preventive maintenance asphalt concrete overlay.  The tack coat shall be uniformly applied with a spray bar paver or a mechanical distributor, except hand spray equipment may be used in areas inaccessible.  The tack coat shall be applied at a temperature recommended by the supplier at a residual rate of 0.14 gallons per square yard +/-0.02 unless otherwise approved by the Engineer.

VI.	PLACEMENT OF HOT MIX ASPHALT

The application rates of the overlay shall range from 80 lbs/sy to 85 lbs/sy in order to result in a ¾” compacted lift thickness.

The thin lift of hot mix asphalt shall be placed by a paver designed for the placement of thin lifts as designated in the contract.  The asphalt mix shall be delivered to the paver hopper at a temperature of 315oF +/- 15oF measured in the paver hopper.  The paver shall be capable of placing the asphalt mix at a speed of 30 feet per minute.  When the base temperature is 500F or above, placement of the asphalt concrete wearing course shall be permitted.

VII.	COMPACTION

Two steel double drum rollers weighing no less than 10 tons shall perform compaction of the asphalt mix.  No less than two passes shall be completed before the surface temperature of the asphalt has reached 185oF.

VIII.	ACCEPTANCE

The Contractor shall perform a gradation, and asphalt cement content on one sample taken in a random manner approved by the Engineer from each 500 tons of production.  The material will be considered acceptable for gradation and asphalt content, if the results obtained are within the tolerance allowed from the job mix formula in the above table.  Material represented by test results outside the tolerance may be removed and replaced with acceptable material by the Contractor at no additional cost to the Department at the discretion of the Engineer.

Should visual examination by the Engineer reveal that the material in any load, or portion of the paved roadway is contaminated, segregated, or flushed with asphalt cement, that load, or portion of the paved roadway may be rejected without additional sampling of the material.

IX.	WARRANTY

The Contractor shall provide a one-year warranty from the date of final acceptance on all thin hot mix asphalt concrete overlay surfaces.  The Department will periodically monitor the overlay surface installed throughout the warranty period for compliance and acceptability.  The Contractor shall repair any area that fails before the end of the warranty period and shall do so within 14 days after Department notification unless otherwise directed by the Department.  Failure of the thin hot mix asphalt concrete overlay surface is defined as the loss of adhesion of the material to the underlying layer resulting in a pothole greater than 1 square foot of area (delamination).  The Engineer shall notify the Contractor of the date for the warranty inspection at the end of the warranty period and the Contractor shall be present at the inspection.

X.	MEASUREMENT AND PAYMENT

Thin hot mix asphalt concrete will be measured in tons and paid for at the contract unit price per ton, which shall include tack coat, surface preparation (except crack and joint sealing), all materials, additives, labor and equipment as described herein to install and complete the work.  Crack and joint sealing will be paid according to the Special Provision for Sealing Cracks in Asphalt Concrete Pavements or Hydraulic Cement Concrete Pavement (Prior to Overlay).

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Thin Hot Mix Asphalt Concrete | Ton |