GUIDELINES — For use on all projects.

SS202-002016-02	September 23, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 202—FINE AGGREGATE

SECTION 202—FINE AGGREGATE of the Specifications is revised as follows:

Section 202.02 – Materials is amended by replacing the first paragraph with the following:

Fine aggregate is classified herein in according to its natural occurrence or method of manufacture as natural sand or stone sand. Natural sand shall consist of grains of hard, sound material, predominantly quartz, occurring in natural deposits or in loosely bound deposits, such as sandstone conglomerate. Stone sand shall consist of sound crushed particles of approved Grade A stone, essentially free from flat or elongated pieces, with sharp edges and corners removed.

Section 202.02 – Materials is amended by inserting the following:

Lightweight aggregate can also be used as a fine aggregate and shall conform to Section 206.

Section 202.03(e) – Deleterious Material is replaced with the following:

Deleterious Material: The amount of deleterious material in sands shall be not more than the following:

| Material | % by Weight | AASHTO Test Method |
| --- | --- | --- |
| Clay lumps | 0.25 | T 112 |
| Shale, mica, coated grains, soft or flaky particles | 1.0 | T 113 |
| Organic material | 0 | T 21 |
| Total material passing No. 200 sieve by washing1,2 |  | T 11 and T 27 |
| For use in concrete subject to abrasion | 3 |  |
| For other concrete | 5 |  |
| 1In the case of stone sand, if the material passing the No. 200 sieve is dust of fracture, essentially free from clay and shale, the percentages shown for use in concrete subject to abrasion and in other concrete may be increased to 5% and 7%, respectively. 2In the case of blends of stone sand and natural sand, provided the natural sand contains no greater than 3% passing the No. 200 sieve for use in concrete subject to abrasion and no greater than 5% for other concrete, then the stone sand limits of 5% and 7% shall apply to the blend. |  |  |