SS204-002016-01	February 22, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 204 – STONE FOR MASONRY, RIPRAP, POROUS BACKFILL, AND GABIONS

SECTION 204 – STONE FOR MASONRY, RIPRAP, POROUS BACKFILL, AND GABIONS of the Specifications is amended as follows:

Section 204.02(c) – Porous backfill is replaced with the following:

Porous backfill shall be No. 78 or 8 aggregate, at least Grade B. Crushed glass meeting the gradation requirements specified in Section 203.02(d) may be directly substituted for No. 78 and 8 aggregates. Lightweight aggregate conforming to Section 206 for coarse aggregate and meeting the 3/4-inch or 1/2-inch grading in AASHTO M 195 may be directly substituted for No. 78 and 8 aggregates.