Guidelines: For use on all projects.

SS206-002016-01	September 23, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFIATIONS

SECTION 206 – LIGHTWEIGHT AGGREGATE

SECTION 206 – LIGHTWEIGHT AGGREGATE is replaced by the following:

206.01 – Description

These specifications cover lightweight aggregate used in the production of hydraulic cement concrete, internally cured concrete using pre-wetted lightweight aggregate, and asphalt surface treatment.

206.02 – Detail Requirements

Lightweight aggregate shall consist of clay, shale, or slate expanded through a sintering or rotary kiln.

The requirements for normal weight aggregate and concrete shall apply to lightweight concrete when a reduced density is specified or when internally-cured concrete (where a portion of the fine aggregate is replaced with pre-wetted lightweight fine aggregate) is specified, except for the following:

- Lightweight aggregate used in hydraulic cement concrete shall conform to AASHTO M 195 and the following requirements.

  - Grading: Gradation for fine and coarse aggregates shall conform to AASHTO M 195. Tests to verify conformance shall be performed in accordance with AASHTO T 27.

  - Soundness: Soundness for fine aggregate shall conform to the freeze and thaw requirements of Table II-2. Soundness for coarse aggregate shall conform to the freeze and thaw requirements of Table II-4. Soundness shall be tested in accordance with AASHTO T 103.

  - Void Content: Void content requirements for fine aggregate shall not apply to lightweight aggregate.

  - Deleterious Material: The amount of deleterious material in fine aggregate shall conform to Section 202 for stone sand. The amount of deleterious material in coarse aggregate shall conform to Section 203.

  - Abrasion Loss: Abrasion loss for coarse aggregate shall conform to the Grade A requirements in Table II-5.

  - Flat and Elongated Particles: Coarse aggregate shall conform to Section 203.

- Lightweight aggregate used for asphalt surface treatment shall conform to AASHTO M 195 except that Sections 3, 6, and 8 will not apply. Grading shall conform to Table II-3 except that the maximum percentage by weight of material passing the No. 8 sieve shall be 16% and passing the No. 16 sieve shall be 9%.