GUIDELINES — For projects requiring SUPERPAVE asphalt concrete.

SS211-002016-03	January 8, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 211 – ASPHALT CONCRETE

SECTION 211 – ASPHALT CONCRETE of the Specifications is amended as follows:

Section 211.01 – Description is replaced with the following:

Asphalt concrete shall consist of a combination of mineral aggregate and asphalt material mixed mechanically in a plant specifically designed for such purpose.

An equivalent single-axle load (ESAL) will be established by the Engineer, and SUPERPAVE mix types may be specified as one of the types listed as follows:

| Mix Type | Equivalent Single-Axle Load (ESAL) Range (millions) | Minimum Asphalt Performance Grade (PG)1 | Aggregate Nominal Maximum Size2 |
| --- | --- | --- | --- |
| SM-9.0A | 0 to 3 | 64S-16 | 3/8 in |
| SM-9.0D | 3 to 10 | 64H-16 | 3/8 in |
| SM-9.0E | Above 10 | 64E-22 | 3/8 in |
| SM-9.5A | 0 to 3 | 64S-16 | 3/8 in |
| SM-9.5D | 3 to 10 | 64H-16 | 3/8 in |
| SM-9.5E | Above 10 | 64E-22 | 3/8 in |
| SM-12.5A | 0 to 3 | 64S-16 | 1/2 in |
| SM-12.5D | 3 to 10 | 64H-16 | 1/2 in |
| SM-12.5E | Above 10 | 64E-22 | 1/2 in |
| IM-19.0A | Less than 10 | 64S-16 | 3/4 in |
| IM-19.0D | 10 to 20 | 64H-16 | 3/4 in |
| IM-19.0E | 20 and above | 64E-22 | 3/4 in |
| BM-25.0A | All ranges | 64S-16 | 1 in |
| BM-25.0D | Above 10 | 64H-16 | 1 in |
| 1Minimum Asphalt Performance Grade (PG) is defined as the minimum binder performance grade for the job mixes as determined by AASHTO T170 or AASHTO M332. 2Aggregate Nominal Maximum Size is defined as one sieve size larger than the first sieve to retain more than 10 percent aggregate. Note: SM = Surface Mixture; IM = Intermediate Mixture; BM = Base Mixture |  |  |  |

Asphalt concrete shall conform to the requirements for the mix type designated on the plans or elsewhere in the Contract for use.

At the Contractor’s option, an approved Warm Mix Asphalt (WMA) additive or process may be used to produce the asphalt concrete (AC) mix type designated.

Table II-13 – Asphalt Concrete Mixtures: Design Range is replaced with the following:

| TABLE II-13 Asphalt Concrete Mixtures: Design Range |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mix Type | Percentage by Weight Passing Square Mesh Sieves |  |  |  |  |  |  |  |  |  |  |
|  | 2 in | 1 1/2 in | 1 in | ¾ in | ½ in | 3/8 in | No. 4 | No. 8 | No. 30 | No. 50 | No. 200 |
| SM-9.0 A,D,E |  |  |  |  | 1001 | 90-100 | 90 max. | 47-67 |  |  | 2-10 |
| SM-9.5 A,D,E |  |  |  |  | 1001 | 90-100 | 58-80 | 38-67 | 23 max |  | 2-10 |
| SM-12.5 A,D,E |  |  |  | 100 | 95-100 | 90 max. | 58-80 | 34-50 | 23 max |  | 2-10 |
| IM-19.0 A,D,E |  |  | 100 | 90-100 | 90 max. | -- | -- | 28-49 |  |  | 2-8 |
| BM-25.0 A,D |  | 100 | 90-100 | 90 max. | -- | -- | -- | 19-38 |  |  | 1-7 |
| C (Curb Mix) |  |  |  |  | 100 | 92-100 | 70-75 | 50-60 | 28-36 | 15-20 | 7-9 |
| 1A production tolerance of 1% will be applied to this sieve regardless of the number of tests in the lot. |  |  |  |  |  |  |  |  |  |  |  |

Table II-14 – Mix Design Criteria is replaced with the following:

| TABLE II-14 Mix Design Criteria |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mix Type | VTM (%) Production | VFA (%) Design | VFA (%) Production | Min. VMA (%) | Fines/Asphalt Ratio | No. of Gyrations N Design |
| SM-9.0A 1,2 | 2.0-5.0 | 75-80 | 70-85 | 17.0 | 0.6-1.3 | 50 |
| SM-9.0D 1,2 | 2.0-5.0 | 75-80 | 70-85 | 17.0 | 0.6-1.3 | 50 |
| SM-9.0E 1,2 | 2.0-5.0 | 75-80 | 70-85 | 17.0 | 0.6-1.3 | 50 |
| SM-9.5A 1,2 | 2.0-5.0 | 75-80 | 70-85 | 16.0 | 0.7-1.3 | 50 |
| SM-9.5D 1,2 | 2.0-5.0 | 75-80 | 70-85 | 16.0 | 0.7-1.3 | 50 |
| SM-9.5E 1,2 | 2.0-5.0 | 75-80 | 70-85 | 16.0 | 0.7-1.3 | 50 |
| SM-12.5A 1,2 | 2.0-5.0 | 73-79 | 68-84 | 15.0 | 0.7-1.3 | 50 |
| SM-12.5D 1,2 | 2.0-5.0 | 73-79 | 68-84 | 15.0 | 0.7-1.3 | 50 |
| SM-12.5E 1,2 | 2.0-5.0 | 73-79 | 68-84 | 15.0 | 0.7-1.3 | 50 |
| IM-19.0A 1,2 | 2.0-5.0 | 69-76 | 64-83 | 14.0 | 0.6-1.3 | 50 |
| IM-19.0D 1,2 | 2.0-5.0 | 69-76 | 64-83 | 14.0 | 0.6-1.3 | 50 |
| IM-19.0E 1,2 | 2.0-5.0 | 69-76 | 64-83 | 14.0 | 0.6-1.3 | 50 |
| BM-25.0A 2,3 | 1.0-4.0 | 67-87 | 67-92 | 13.0 | 0.6-1.3 | 50 |
| BM-25.0D 2,3 | 1.0-4.0 | 67-87 | 67-92 | 13.0 | 0.6-1.3 | 50 |
| 1Asphalt content should be selected at 4.0% air voids for A & D mixes, 3.5% air voids for E mix. 2Fines-asphalt ratio is based on effective asphalt content. 3Base mix shall be designed at 2.5% air voids. BM-25A shall have a minimum asphalt content of 4.4% unless otherwise approved by the Engineer. BM-25D shall have a minimum asphalt content of 4.6% unless otherwise approved by the Engineer. |  |  |  |  |  |  |

Section 211.04(e)4 – Type E(HP) asphalt mixtures is inserted as follows:

Type E(HP) asphalt mixtures shall consist of mixes incorporating a neat asphalt material with a high polymer modification (approximately 7.5%) complying with AASHTO M332 for PG 76E-28(HP) with the exception that Multiple Stress Creep and Recovery (MSCR) shall have a Jnr3.2 maximum value of 0.1 kPa-1 when tested according to AASHTO T350. The minimum MSCR % recovery at 3.2 kPa shall be 90%. The MSCR test for Jnr and % recovery shall be run at 76°C. The viscosity shall be less than or equal to 3.0 Pa-s, however the Engineer may increase this limit to 5.0 Pa-s if the binder supplier and contractor agree that the binder is suitably workable. HP designated mixtures shall not contain more than 15% RAP material.

Section 211.05 – Testing is amended by deleting the eighth and ninth paragraphs.

Section 211.08 – Acceptance is amended by replacing the sixth paragraph with the following:

Asphalt content will be measured as extractable asphalt or weight after ignition.  The Contractor shall submit a copy of burn tickets from an ignition oven to the Engineer and all the original tickets shall be available upon Engineer’s request.  Original tickets shall be maintained on file by the Contractor for a period of 5 years or until final acceptance of the applicable contract, whichever is greater.