GUIDELINES — For use on all projects.

SS223-002016-03	July 3, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 223 – STEEL REINFORCEMENT

SECTION 223 – STEEL REINFORCEMENT of the Specifications is amended as follows:

Section 223.02(a)3 – Welded wire fabric is raplaced with the following:

Welded wire fabric shall conform ASTM A1064. When used in continuously reinforced hydraulic cement concrete pavement wire fabric shall be deformed, furnished in flat sheets, and shall conform to ASTM A497, high yield of 70,000 psi.

Section 223.02(e) – Corrosion Resistant Reinforcing Steel, Class I is replaced with the following:

Corrosion Resistant Reinforcing Steel, Class I shall conform to AASHTO M 334M/M 334-17 Type 1035 CS with a minimum chromium content of 9.2% or UNS (Unified Numbering System for Metals and Alloys) Designation: S24100.

Section 223.02(f) – Corrosion Resistant Reinforcing Steel, Class II is replaced with the following:

Corrosion Resistant Reinforcing Steel, Class II shall conform to AASHTO M 334M/M 334-17. UNS Designation: S32101.

Section 223.02(g) – Corrosion Resistant Reinforcing Steel, Class III is replaced with the following:

Corrosion Resistant Reinforcing Steel, Class III shall conform to AASHTOM 334M/M 334-17 . UNS Designations: S24000, S30400, S31603, S31653, S31803, and S32304.