Guidelines: For use on all projects.

SS226-002016-01	September 27, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 226 – STRUCTURAL STEEL

SECTION 226 – STRUCTURAL STEEL of the Specifications is amended as follows:

Section 226.02(c) – Anchor Bolts is replaced with the following:

Anchor bolts shall conform to AASHTO M 314 or ASTM F1554.

1.	Anchor bolts for general use shall be Grade 36. Nuts and washers shall conform to ASTM A563 and ASTM F844 respectively. Threads shall be coarse series.

2.	High-strength anchor bolts shall conform to ASTM F1554, Grade 55 or AASHTO M314, Grade 55, with supplemental requirements of S1. Nuts and washers shall conform to ASTM A563, Grade DH and ASTM F436 respectively.

3.	Galvanization of steel anchor bolts, nuts, and washers shall conform to ASTM A153.

4.	Anchor bolts for railings shall conform to (c)1 herein, and shall be hot-dipped galvanized.

Section 226.02(h) – High-Strength Bolts, Nuts, Washers, and Direct Tension Indicators is renamed High-Strength Bolts and replaced with the following:

High-Strength Bolts shall conform to ASTM F3125 Grade A325 Type 1, unless specified otherwise. Nuts, Washers, and Direct Tension Indicators (DTIs) shall conform to specifications appropriate for the grade and type of bolt according to the table below. All nuts shall be Heavy Hex, and all washers shall be Hardened.

| High-Strength Bolts | Nuts | Washers | DTIs |
| --- | --- | --- | --- |
| ASTM F3125, Grade A325, Type 11 | ASTM A563, Grade DH | ASTM F436 | ASTM F959 |
| ASTM F3125, Grade A325, Type 3 | ASTM A563, Grade DH3 | ASTM F436 | ASTM F959 |
| ASTM F3125, Grade A490, Type 1 | ASTM A563, Grade DH ASTM A194, Grade 2H | ASTM F436 | ASTM F959 |
| ASTM F3125, Grade A490, Type 3 | ASTM A563, Grade DH3 | ASTM F436 | ASTM F959 |
| ASTM A449, Type 11 | ASTM A563, Grade DH | ASTM F436 | ASTM F959 |
| ASTM A449 Type 3 | ASTM A563, Grade DH3 | ASTM F436 | ASTM F959 |
| 1All bolts conforming to ASTM F3125, Grade A325, Type 1 or ASTM A449, Type 1 and their nuts, washers, and DTIs shall be galvanized. |  |  |  |

  - Bolts, nuts, and washers conforming to ASTM F3125 Grade A490 shall not be galvanized. High-strength bolts used with unpainted weathering steel shall conform to ASTM F3125 Grade A325, Type 3; ASTM A449, Type 3; or, when specified, ASTM F3125 Grade A490, Type 3. All use of high-strength bolts conforming to ASTM A449 shall be approved, in writing, by the Engineer. ASTM A449 bolts shall conform to the rotational capacity testing requirement in ASTM F3125 Grade A325 and these Specifications.

  - The maximum hardness for bolts conforming to ASTM F3125 Grade A325 shall be 33Rc. The maximum tensile strength for such bolts shall be 150 kips per square inch for bolts 1 inch or less in diameter and 120 kips per square inch for larger bolts.

  - High-strength fasteners (plain and coated) shall pass a rotational-capacity test as detailed in VTM 135.

    - Bolts shall be proof-load tested in accordance with ASTM F606, Method I. Full-size bolts shall be wedge tested in accordance with ASTM F606. Nuts shall be proof-load tested in accordance with ASTM F606. Galvanized bolts shall be wedge tested after galvanizing. Galvanized nuts shall be proof-load tested in accordance with ASTM F606 only after overtapping, galvanizing, and lubricating operations are completed.

    - Galvanized bolts, nuts and washers shall be hot-dipped galvanized in accordance with ASTM A153. The Contractor may use mechanically galvanized bolts, nuts, and washers that conform to ASTM B695, Class 50 if the bolts are to be topcoated with paint.

When galvanized nuts conforming to ASTM A563 are specified, the amount of over-tapping may be less than specified; however, all nuts in each lot shall be over-tapped by the same amount. Galvanized nuts shall be lubricated in accordance with ASTM A563 using a lubricant sufficiently tinted so as to be readily visible.

Galvanized bolts, nuts, and washers shall have the galvanization measured for thickness. Measurements for bolts shall be taken on the wrench flats or top of the bolt head. Measurements for nuts shall be taken on the wrench flats.

When galvanized washers are specified, hardness testing shall be performed after galvanizing. The coating shall be removed prior to testing.

    - All bolts, nuts, and washers shall be furnished with a marking that readily identifies their manufacturer. The Contractor shall provide the Engineer with an example of such marking and the manufacturer’s certification for each bolt, nut, and washer supplied to the project. The Contractor shall ensure that two samples from each rotational capacity lot, each sample consisting of one bolt, nut, washer, and DTI (if used on the project), are submitted to the Department for testing, and are accompanied by all documentation.

Documentation shall indicate the results of all tests and processes performed on the hardware, the name of the testing facility, address where the tests were performed and the date of testing. Test results of bolts and nuts shall also indicate the lot number of the product. Bolts, nuts, and washers from different rotational-capacity lots shall not be shipped in the same container. In addition, shipping containers shall be marked with the rotational-capacity test lot number of the product supplied.

Section 226.02(i) – Steel Plate is inserted as follows:

Steel plate shipped to the project site as plate shall have the direction of roll indicated on the plate to provide direction to the field for cutting along the appropriate axis when making components in the field. The plate shall be blast cleaned to either SSPC SP-6 or SP-10 finish and have an arrow painted along the direction of roll with the letters “DOR” above it using an inorganic zinc rich primer from the Department’s Approved List 13.