GUIDELINES — For projects requiring pipe and pipe arches.

SS232-002016-03	May 21, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 232—PIPE AND PIPE ARCHES

SECTION 232—PIPE AND PIPE ARCHES of the Specifications is amended as follows:

Section 232.02(c)1 – Corrugated steel culvert pipe and pipe arches is replaced with the following:

Corrugated steel culvert pipe and pipe arches shall conform to AASHTO M36 except that helically formed pipe shall be tested in accordance with AASHTO T249 at the rate of one test per week per corrugation machine per work shift.  The Contractor shall maintain records of such test for a period of 24 months.  Pipe shall be fabricated from materials conforming to AASHTO M218 for galvanized pipe, AASHTO M274 for aluminum coated pipe, AASHTO M246 for polymer coated pipe and AASHTO M289 for aluminum zinc alloy coated pipe.  Steel spiral rib pipe shall be of smooth wall spiral rib construction.  When connecting bands or flared end sections are required, helically formed pipe shall have rerolled ends with a minimum of two annular corrugations.  End sections shall be produced in accordance with AASHTO M36 from materials conforming to the applicable requirements of AASHTO M218 for use with galvanized pipe, AASHTO M274 for use with aluminum-coated or polymer coated pipe, or AASHTO M289 for use with aluminum zinc alloy-coated pipe.

Joints shall be installed as specified on the plans, in the event the joint is not specified, it shall be a Silt-Tight joint.

Section 232.02(c)4a – Steel encasement pipe is replaced with the following:

Steel encasement pipe shall conform to ASTM A139 or ASTM A53 with a minimum wall thickness of 0.500 inch and shall have beveled edges suitable for welding or be threaded. The hydrostatic test for such pipe will not be required.

Section 232.02(c)7 – Concrete-lined corrugated steel pipe is deleted, and paragraphs 8 and 9 are renumbered to 7 and 8, respectively.

Section 232.02(l) – Polypropylene (PP) Pipe is replaced with the following:

Polypropylene (PP) Pipe: PP corrugated culvert and storm drain pipe and its fittings and joining systems shall conform to AASHTO M330. Pipes with nominal diameters of 12 inches through 30 inches, inclusive, shall be Type S (double-wall). Pipes with nominal diameters of 36 inches through 60 inches, inclusive, shall be Type S or Type D (triple-wall). The Department will not permit the use of PP less than 12 inches or greater than 60 inches in nominal diameter.

Section 232.02(m) – Pipe Joints is inserted as follows:

Pipe joints shall meet the requirements of AASHTO R 82 for Soil-Tight, Silt-Tight, Leak-Resistant or other special design, except that leak-resistant joints shall not require infiltration or exfiltration testing in the field, and joints shall be on VDOT Materials Division Approved List for pipe joints.  Pipe Joint systems shall be submitted to the Materials Division certifying the system meets the requirements for Soil-Tight, Silt-Tight, Leak-Resistant or Special Design in order to be on the approved list.

Section 232.02(n) – Pipe to Structure Connections and Waterstops is inserted as follows:

Manufactured pipe connection systems for connecting pipe to drainage structures shall be submitted to the Materials Division certifying the system meets the requirements for Soil-Tight, Silt-Tight, or Leak-Resistant in order to be on the approved list.  When resilient connectors for silt tight connections are specified for concrete pipe to concrete structures, the connectors shall meet the requirements of ASTM C1478.  When resilient connectors for leak resistant connections are specified for flexible pipe to concrete structures, the connectors shall meet the requirements of ASTM F2510.

When waterstops are specified, they shall meet the requirements of ASTM F2510, Section 4.1 Materials and Manufacture and Section 4.2 Mechanical Devices.  The waterstop shall have a 1 inch minimum keylok anchor embedded into the concrete or mortar connection on pipe sizes below 18 inch diameter and 1.5 inch for pipe 18 inches and greater in diameter.  There shall be a minimum 2 inches of concrete or mortar connection around the rubber gasket to permit proper consolidation around the gasket.  All waterstops shall be secured to the pipe with a take-up clamp before applying mortar.