Guidelines - For use on all projects with roadside development materials.

SS244-002016-02	April 15, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2016 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 244 – ROADSIDE DEVELOPMENT MATERIALS

SECTION 244 – ROADSIDE DEVELOPMENT MATERIALS of the Specifications is amended as follows:

Section 244.02(b) – Topsoil is amended by replacing the first paragraph with the following:

Topsoil may be naturally occurring or may be manufactured and shall be free of foreign objects such as refuse, woody vegetation, stumps, roots, brush, stone larger than 3/4 inches, viable noxious weeds or weed seed, plant propagules, and any other material toxic or deleterious to plant growth. Maximum size of other foreign objects shall be 2 inches. Topsoil shall conform to the following:

Section 244.02(b)1 – Class A topsoil is replaced by the following:

Class A topsoil shall be stockpiled topsoil that has been salvaged from within the project limits in accordance with Section 303.04(a). It shall be the original layer of the soil profile formed under natural conditions, and its physical, chemical, and biological characteristics shall be consistent with the “A” horizon soil profile as defined by the United States Department of Agriculture–Natural Resources Conservation Service (USDA–NRCS) Soil Survey Division.

Section 244.02(b)2 – Class B topsoil is amended by replacing the first paragraph with the following:

Class B topsoil shall be topsoil furnished from sources outside the project limits and shall be either the original top layer of a soil profile formed under natural conditions, or manufactured top soil. Regardless of the source, all topsoil shall have the physical, chemical, and biological characteristics consistent with the “A” horizon soil profile as defined by USDA–NRCS Soil Survey Division, If the topsoil is not manufactured topsoil, then it shall consist of natural, friable, loamy soil without admixtures of subsoil or foreign materials. The Contractor shall provide to the Engineer a source of materials for topsoil planned for use on the project prior to use.

Section 244.02(l) – Rolled Erosion Control Products is replaced by the following:

Rolled Erosion Control Products:

1.	Rolled Erosion Control Products (Standard EC-2) shall conform to Table II-22C and the following requirements. EC-2 products shall be designed for use on geotechnically stable slopes and channels as detailed herein.

a.	EC-2, Type 1 shall be a relative short-term single-net erosion control blanket or open weave textile. EC-2, Type 1 shall be one of the following materials: (1) an erosion control blanket composed of processed degradable natural or polymer fibers mechanically-bound together by a single degradable synthetic or natural fiber netting to form a continuous matrix; or (2) an open weave textile composed of processed degradable natural or polymer yarns or twines woven into a continuous matrix. EC-2, Type 1 shall typically have a 12-month functional longevity from the date of installation and be designed for shear stresses up to 1.50 pounds per square foot, for use on up to 1V:3H slopes and channels.

b.	EC-2, Type 2 shall be a relative short-term double-net erosion control blanket. The blanket shall be composed of processed natural or polymer fibers mechanically bound between two natural fiber or synthetic nettings to form a continuous matrix. EC-2, Type 2 materials shall typically have a 12-month functional longevity from the date of installation and be designed for shear stresses up to 1.75 pounds per square foot, for use on up to 1V:2H slopes and channels.

c.	EC-2, Type 3 shall be an extended term erosion control blanket or open weave textile. EC-2, Type 3 blankets shall be one of the following materials: 1) an erosion control blanket composed of processed slow degrading natural or polymer fibers mechanically-bound together between two slow degrading synthetic or natural fiber nettings to form a continuous matrix; or 2) an open weave textile composed of processed slow degrading natural or polymer yarns or twines woven into a continuous matrix. EC-2, Type 3 material shall typically have a 24-month functional longevity from the date of installation and be designed for shear stresses up to 2.00 pounds per square foot, for use on slopes up to 1V:1.5H and channels.

d.	EC-2 Type 4 shall be a long-term erosion control blanket or open weave textile. EC-2, Type 4 blankets shall be one of the following materials: (1) an erosion control blanket composed of processed slow degrading natural or polymer fibers mechanically-bound together between two slow degrading synthetic or natural fiber nettings to form a continuous matrix; or (2) an open weave textile composed of processed slow degrading natural or polymer yarns or twines woven into a continuous matrix. EC-2, Type 4 material shall typically have a 36-month functional longevity from the date of installation and be designed for shear stresses up to 2.25 pounds per square foot, for use on up to 1V:1H slopes and channels with.

2.	Permanent Rolled Erosion Control Products (Standard EC-3) shall be permanent turf reinforcement mats conforming to Table II-22D and the following:

a.	EC-3, Type 1 shall be a non-degradable mat of sufficient thickness, strength and void space for permanent erosion protection and vegetation reinforcement on geotechnically stable slopes with gradients up to 1V:1.5H, channels with design shear stresses up to 6.0 pounds per square foot, and on other areas where design flow conditions exceed the limits of sustainability for mature natural vegetation.

b.	EC-3, Type 2 shall be a non-degradable mat with sufficient thickness, strength and void space for permanent erosion protection and vegetation reinforcement on geotechnically stable slopes with gradients up to 1V:1H, channels with design shear stresses up to 8.0 pounds per square foot, and other areas where design flow conditions exceed the limits of sustainability for mature natural vegetation.

c.	EC-3, Type 3 shall be a non-degradable mat with sufficient thickness, strength and void space for permanent erosion protection and vegetation reinforcement for use on geotechnically stable slopes up to 1V:0.5H, channels with design shear stresses up to 10.0 pounds per square foot, and other areas where design flow conditions exceed the limits of sustainability for mature natural vegetation.

Section 244.02(o) – Sediment Tubes is replaced with the following:

Sediment Tubes shall be composed of compacted material such as certified 100% weed free curled excelsior wood with 80% of the fiber being at least 4 inches in length, natural coconut fibers (bristle and mattress form obtained from freshwater cured coconut husk.), certified 100% weed free agricultural straw, certified 100% weed free hardwood mulch, or a mix of these materials or other VDOT-accepted materials enclosed by a tubular flexible outer netting material consisting of one of the following:

- Seamless, photo-degradable, high-density, polyethylene, polyester, or ethyl vinyl acetate,  treated with ultraviolet stabilizers.

- Seamless, non-degradable, high-density polyethylene.

- Seamless, non-degradable, high-density polypropylene.

- Coir netting or coir fastening twine.

Sediment tubes of washed shredded recycled rubber particles with a minimum of 98% of metal removed contained in seamless, non-degradable, high-density polypropylene may be used for Inlet Protection and Temporary Check Dams in accordance with the Standard Drawings.

Straw, curled excelsior wood, or natural coconut products that are rolled up to create a sediment tube without an outer netting will not be allowed. Natural pine needles, leaf mulch, and grass clipping-filled sediment tubes will not be permitted.