cq217-000100-00

Guidelines: For use on all projects where concrete is used.

DENSITY OF LIGHTWEIGHT CONCRETE

Section 217.12(b) is amended by replacing the third paragraph with the following:

Maximum density of freshly mixed lightweight concrete, when tested according to ASTM C138, shall be 120 lbs/ft³, or as specified on the Plans.

3-5-19 (SPCN)