Guidelines: For use on all Latex and THMACO projects where inlaid pavement markers will be installed.

SEALING GROOVES FOR INLAID PAVEMENT MARKERS  — The Contractor shall coat the entire groove area for Inlaid Pavement Markers with liquid asphalt coating (emulsion) conforming to Section 315.02(e) of the Specifications using a pressure distributor following the cutting and cleaning of the depressions of waste material. The approximate application rate shall be 0.1 gallons per square yard. The application temperature shall be between 160°F and 180°F.

The Contractor shall cover and protect the retroreflector during this operation. Any dirty or damaged retroreflectors or pavement markings that can’t be cleaned by brushing them off shall be replaced. Waste material resulting from the operation shall be removed from the paved surface and shall not be disposed of where waterways may be at risk of contamination.

Liquid Asphalt Coating (Pavement Marker Groove) will be measured in square yards of groove and paid for at the Contract square yard price. This price shall include cleaning the groove prior to application of the coating and furnishing and applying coating as specified herein.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Liquid Asphalt Coating (Pavement Marker Groove) | Square yard |

10-24-19 (SPCN)