cq317-000100-00

GUIDELINES — For projects requiring Stone Matrix Asphalt. Include SS248-002016-01.

SECTION 317—STONE MATRIX ASPHALT CONCRETE PLACEMENT of the Specifications is amended as follows:

317.08—Compaction is amended to replace the second paragraph with the flowing:

The Contractor shall approach the use of vibratory rollers on SMA with caution to minimize coarse aggregate fracture/breakage in the aggregate skeleton of SMA mixes. If the Contractor elects to use a vibratory roller, the mat should receive not more than three vibratory passes. The Contractor shall use the roller only on the highest frequency and lowest amplitude setting.

9-17-18 (SPCN)